SPECIFICATIONS

CONNETTORE 20 e 38 IN ACCIAIO

Supply and installation of a mechanical steel peg connector with electrolytic galvanisation, upper circular washer, lower movable washer and threaded shank.

The product must be used for:

- Connection between existing structures and new waterproofing protective and/or confinement slabs (e.g. fibre-reinforced concrete)

- Anchoring to mortar supports or concrete castings

The material must have the following characteristics:

CONNETTORE 20

Specification, Values

Nominal diameter of head washer: 22.0 mm

Nominal thickness of head washer: 4.0 mm

Total length of connector: 80.0 mm

Insertion length: 60.0 mm

Threaded section length: 60.0 mm

Protruding section length: 20.0 mm

Nominal diameter of shank: 10.5 mm

Resistant diameter of shank: 7.2 mm

Characteristic tensile strength: 32.7 kN

Characteristic shear strength: 16.3 kN

CONNETTORE 38

Steel shank

Specification, Values

Total length of connector: 185.0 mm

Insertion length: 147.0 mm

Threaded section length: 117.0 mm

Protruding section length: 38.0 mm

Nominal diameter of shank: 13.0 mm

Resistant diameter of shank: 12.1 mm

Characteristic tensile strength: 36.2 kN

Characteristic shear strength: 24.1 kN

Head washer steel

Specification, Values

Nominal diameter of head washer: 50.0 mm

Nominal thickness of head washer: 6.0 mm

Characteristic yield strength: 178.5 Mpa

Characteristic breaking strength: 440.0 Mpa

as well as Connettore 20 and 38 Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.

EN Specifications n. FN02-FN03 | CP | 02 | 00 | W | 01/26