**SPECIFICATIONS**

 WT BREAK

Supply and installation of a self-sealing watertight box element designed to determine and guide the contraction phenomena of reinforced concrete structures and seal the cracks that will form in its correspondence.

The product must be used on reinforced concrete walls, made continuously such as: masonry in contact with the ground in general, tanks, purifiers, retaining walls, etc.

The material must have the following characteristics:

**Specification and Values**

**Thickness:** 20 mm

**Width:** 185 mm

**Length:** 1.000 mm

**Hydro-expansive profile composition:**25% butyl rubber; 75% Sodium Bentonite

as well as Wt Break Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website [www.volteco.com.](http://www.volteco.com/)

EN Specifications n. BC | CP | 01 | 00 | W | 06/24

