**SPECIFICATIONS**

BENTONITE SODICA NATURALE

Supply and installation of granular sodium bentonite used dry or pre-hydrated for accurate waterproofing reinforcements.

The product will need to be used to fill cavities or gaps in the substrate before installing the waterproofing membrane/system.

The material must have the following characteristics:

**Specification, Test method, Values**

**Smectite Content, XRD:** Min 75%

**Fluid Loss, ASTM D 5891:** 18 ml Max

**Free swelling, ASTM D 5890:** > 24 ml/2g Min

as well as Bentonite Sodica Naturale Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and / or be subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website [www.volteco.com](http://www.volteco.com).

EN Specifications n. DB | CP | 00 | 00 | W | 08/25

