
AKTI-VO BS

Supply and installation of mastic, composed of natural sodium Bentonite and butyl rubber, suitable for the waterproof sealing of penetrations, for the connection between elements of different nature or for the grouting of the VOLGRIP bentonite membrane.

The product must be used for:
· Accurate sealing of connection reinforcing bars, such as connectors, reinforcing bars, anchoring brackets, etc.
· Seal penetrations, such as cement, metal and plastic pipes embedded into the reinforced concrete, pole heads and pumping wells
· Connection fillet between discontinuous elements
· Reinforcement of the connection between the Volgrip bentonite membrane and other waterproofing
· Grouting of the Volgrip bentonite membrane in tears or joint



The material must have the following characteristics:


Specification and Values

Appearance: Dark grey gel
Specific weight: 1.5 kg/l
Mixture composition (in weight):	50% Sodium bentonite
50% non-toxic plasticizing agents


as well as Akti-vo Bs Volteco or a product with equal or superior characteristics.
The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.
For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.
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