AQUASCUD LINE

Supply and installation of a painted aluminium draining drip profile for finishing and perimeter protection of terraces and balconies, to promote a correct water drainage.

The product must be used in correspondence with the fronts of terraces, balconies and roofing structures in general with a finish along the edge of the surface.

The material must have the following characteristics:

Specification and Values

Composition: aluminium

Thickness: 1.5 mm

Paint: With UV-resistant polyester powders

Fastening holes: 2.5 mm diameter

Outflow holes for H.10 version: every 10 cm - length 10 mm – width 4 mm

as well as Aquascud Line Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.

EN Specifications n. CF01-CF02-CF03 | CP | 01 | 01 | W | 07/26