AQUASCUD REFLEX

Supply and installation of solvent-free, ready-to-use, cold-cured, elastic, waterproofing coating based on acrylic resins in water emulsion, ready to use and applied cold, this glossy off-white coating is characterised by high solar reflectance (Solar Reflectance Index - SRI) and is classified as BROOF(t2) for external fire behaviour in accordance with standard EN 13501-5.

The product shall be used and applied in two cross coats, 12 hours apart, at a total application rate of 1.6 to 2.0 kg/m², depending on the type and porosity of the substrate.

The material must have the following characteristics:

Certification according to UNI EN 11928 Standard

CE certification in accordance with the UNI EN 13501-5 Broof(T2) standard

Initial requirements UNI 11928-1:2023

Feature, Test method, Performance requirements, Declared performance

Reaction to fire (UNI EN 13501-1): Declared Euroclass / Euroclass E

Watertightness (water passage with 60 KPa), UNI EN 1928: No passage / No passage

Water vapour transmission properties (UNI EN ISO 7783): Class / Class I

Direct tensile adhesion, concrete type MC (0,40), UNI EN 1542: ≥ 0.5 N/mm² / ≥ 1.0 N/mm²

Impact resistance (UNI EN 6272-1): Class / Class III

Static punching (UNI EN 12730): Maximum value > 50 N / ≥ 50 N

Dynamic crack bridging (23°C), UNI EN 1062-7: Class B2 / Class B4.1

Dynamic crack bridging at low temperatures (-10°C), UNI EN 1062-7: Class B1 / Class B2

Slipping resistance (UNI EN 13036-4): Class / Class II

Capillary absorption (UNI EN 1062-1): W ≤ 0.1 Kg/m²*h⁻⁰·⁵ / W ≤ 0.1 Kg/m²*h⁻⁰·⁵

Durability UNI 11928-1:2023

Feature, Test method, Performance requirements, Declared performance

Heat ageing resistance 7 days at 70±3°C (Watertightness), point 4.1 of UNI EN 1062-11:2003: No passage / No passage

Acceptance criteria after exposure (UNI EN ISO 4628-2, UNI EN ISO 4628-4, UNI EN ISO 4628-5): No swelling, No cracking, No spalling / No swelling, No cracking, No spalling

Frost/thaw Without thawing salts 20 cycles (Adhesion to substrate), UNI EN 13687-3: ≥ 0.5 N/mm² / ≥ 1.0 N/mm²

Acceptance criteria after exposure (UNI EN ISO 4628-2, UNI EN ISO 4628-4, UNI EN ISO 4628-5): No swelling, No cracking, No spalling / No swelling, No cracking, No spalling

UV (400 MJ/m², 2460 hours) and Spray (492 hours), UNI EN ISO 4892-3: - / -

Acceptance criteria after exposure (UNI EN ISO 4628-2, UNI EN ISO 4628-4, UNI EN ISO 4628-5): No swelling, No cracking, No spalling / No swelling, No cracking, No spalling

Hazardous substances: See safety data sheets

The quoted data are obtained in an laboratory at +20°C and 60% RH.

EN Specifications n. CB14-CB15-CB16 | CP | 00 | 01 | W | 07/26

Feature, Test method, Certified performance (**)

Solar Reflectance Index (SRI) (ASTM E1980-11): 98,7

Feature, Test method, Classification method, Certified performance (**)

Fire resistance classification, UNI CEN/TS 1187:2012 -Test 2, UNI EN 13501-5:2016: BROOF (T2)

as well as Aquascud Reflex Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and / or be subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.

EN Specifications n. CB14-CB15-CB16 | CP | 00 | 01 | W | 07/26