AQUASCUD REFLEX

Supply and installation of solvent-free, ready-to-use, cold-cured, elastic, waterproofing coating based on acrylic resins in water emulsion, ready to use and applied cold, this glossy off-white coating is characterised by high solar reflectance (Solar Reflectance Index - SRI) and is classified as BROOF(t2) for external fire behaviour in accordance with standard EN 13501-5.

The product shall be used and applied in two cross coats, 12 hours apart, at a total application rate of 1.6 to 2.0 kg/m², depending on the type and porosity of the substrate.


The material must have the following characteristics:
Certification according to UNI EN 11928 Standard
CE certification in accordance with the UNI EN 13501-5 Broof(T2) standard


Initial requirements UNI 11928-1:2023
Feature, Test method, Performance requirements, Declared performance

Reaction to fire (UNI EN 13501-1): Declared Euroclass / Euroclass E
Watertightness (water passage with 60 KPa), UNI EN 1928: No passage / No passage
Water vapour transmission properties (UNI EN ISO 7783): Class / Class I
Direct tensile adhesion, concrete type MC (0,40), UNI EN 1542: ≥ 0.5 N/mm² / ≥ 1.0 N/mm²
Impact resistance (UNI EN 6272-1): Class / Class III
Static punching (UNI EN 12730): Maximum value > 50 N / ≥ 50 N
Dynamic crack bridging (23°C), UNI EN 1062-7: Class B2 / Class B4.1
Dynamic crack bridging at low temperatures (-10°C), UNI EN 1062-7: Class B1 / Class B2
Slipping resistance (UNI EN 13036-4): Class / Class II
Capillary absorption (UNI EN 1062-1): W ≤ 0.1 Kg/m²*h⁻⁰·⁵ / W ≤ 0.1 Kg/m²*h⁻⁰·⁵


Durability UNI 11928-1:2023
Feature, Test method, Performance requirements, Declared performance

Heat ageing resistance 7 days at 70±3°C (Watertightness), point 4.1 of UNI EN 1062-11:2003: No passage / No passage
Acceptance criteria after exposure (UNI EN ISO 4628-2, UNI EN ISO 4628-4, UNI EN ISO 4628-5): No swelling, No cracking, No spalling / No swelling, No cracking, No spalling
Frost/thaw Without thawing salts 20 cycles (Adhesion to substrate), UNI EN 13687-3: ≥ 0.5 N/mm² / ≥ 1.0 N/mm²
Acceptance criteria after exposure (UNI EN ISO 4628-2, UNI EN ISO 4628-4, UNI EN ISO 4628-5): No swelling, No cracking, No spalling / No swelling, No cracking, No spalling
UV (400 MJ/m², 2460 hours) and Spray (492 hours), UNI EN ISO 4892-3: - / -
Acceptance criteria after exposure (UNI EN ISO 4628-2, UNI EN ISO 4628-4, UNI EN ISO 4628-5): No swelling, No cracking, No spalling / No swelling, No cracking, No spalling
Hazardous substances: See safety data sheets
The quoted data are obtained in an laboratory at +20°C and 60% RH.
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Feature, Test method, Certified performance (**)

Solar Reflectance Index (SRI) (ASTM E1980-11): 98,7


Feature, Test method, Classification method, Certified performance (**)

Fire resistance classification, UNI CEN/TS 1187:2012 -Test 2, UNI EN 13501-5:2016: BROOF (T2)


as well as Aquascud Reflex Volteco or a product with equal or superior characteristics.
The technical data must be supported by test certification issued by an accredited official laboratory and / or be subjected to quality control according to ISO 9001.
For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.
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