BI MORTAR LEVELLING SEAL

Supply and installation of shrinkage-compensated pourable grout ideal for applications demanding both waterproofing and high-resistance performance.

It can be used without additions or, for the execution of high thickness castings, it can be integrated with gravel (weight from 6 to 16 mm) up to 30% by weight.

The product must be used for:

• Structural reintegration of columns and beams by casting in formworks

• Fixing of anchoring and metal structures

• Fixing of anchor bolts of metal rails of gates, cranes and machinery in general

• Filling of rigid joints between precast elements

• Rebuilding of pile heads and diaphragm walls

• Refurbishing of reinforced concrete of industrial, road, airport, and car park floors

• Horizontal refurbishment castings (e.g. slabs of lift pits, light-shafts, tanks, etc.) even in case of reduced thicknesses and/or negative water pressure conditions

The material must have the following characteristics:

EC Certification according to UNI EN 1504-3:2006 and UNI EN 1504-6:2006

Specification, Test method, Values

Compressive strength after 28 days (UNI EN 12190): 72.5 MPa

Flexural strength after 28 days (UNI EN 12190): 11.9 MPa

Adhesion to the concrete (UNI EN 1542): 3.5 MPa

Compressive modulus of elasticity after 28 days (UNI EN 13412): 28.5 MPa

Resistance to carbonation (dk < control concrete (0.45 MC) UNI EN 13295: Fulfilled requisite

Thermal compatibility Part 1 (adhesion after 50 un/freezing cycles) UNI EN 13687-1: 2.8 MPa

Thermal compatibility Part 2 (adhesion after 30 thunder cycles) UNI EN 13687-2: 2.83 MPa

Thermal compatibility Part 4 (adhesion after 30 dry thermal cycles) UNI EN 13687-4: 3.1 MPa

Slipping resistance (UNI EN 13036-4): Dry: class II; Wet: class I

Pull-out strength of steel bars - displacement at 75 kN load (UNI EN 1881): 0.35 mm

Reaction to fire (UNI EN 13501-1): Euroclass A1

Feature, Certifying body, Test method and Certified performance

Impermeability, IMM SA (Switzerland), UNI 12390-8: 7 Bar no passage

Radon diffusion coefficient, CZECH TECHNICAL UNIVERSITY IN PRAGUE, ISO/TS 11665-13: 6.5 E-9 m²/s

as well as Bi Mortar Levelling Seal Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.

EN Specifications n. IL10 | CP | 02 | 00 | W | 07/26