CP0

Supply and installation of a thick, coloured, organic mineral finish paste-coating for outdoor and indoor use, featuring high breathability and water resistance, composed of water-dispersed acrylic-siloxane resins.
The coating must be applied according to the indications of the technical data sheet according to the chosen particle size.

The product must be used in the protection and finishing of walls in general, both indoors and outdoors.



The material must have the following characteristics:
EC Certification according to EN 15824


Specification, Test method and Values

Bond strength (UNI EN 1542): ≥ 0.3 MPa
Capillary absorption (UNI EN 1062-3): W = 0.079 kg*m-2²*h-0.5⁰·Class W3 (low permeability)
Water vapour permeability (UNI EN 7783-2 – equivalent Sd): Sd ≤ 0.6472 Class V2 (average)
Thermal conductivity (UNI EN 1745): 10, dry = 0.83 W/mK (P = 50%) λ10, dry = 0.93 W/mK (P = 90%)
Crack Bridging Ability (product only) for size 1.0 - 1.2 - 1.5 (UNI EN 1062-7 – static method): 0.43 mm (Class A2 > 0.25 mm)
Crack Bridging Ability (CP1 + Flexonet mesh+CP0 pack) (UNI EN 1062-7 - static method): 1.51 mm (Class A4 > 1.25 mm)
Crack Bridging Ability (CP1 + Xnet mesh+CP0) (UNI EN 1062-7 - static method): 0.7 mm (Class A3 > 0.5 mm)


Specification, Category, Test method and Values, Declared performance

VOC content, CAT. C - BA paints for outside mineral support walls Maximum limit: 20 g/l (Direttiva 42/2004/EC): 19 g/l


as well as CP0 Volteco or a product with equal or superior characteristics.
The technical data must be supported by test certification issued by an accredited official laboratory and / or be subjected to quality control according to ISO 9001.
For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.
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