FLEXOMIX 30

Supply and installation of cement-based modified polymer mortar with a low modulus of elasticity, thixotropic and fibre-reinforced that allows volume restoration and surface finishing of concrete or plaster in a single solution, applied in layers not exceeding 2 cm depending on the type of use.

The product must be used for:

- To level the surface of deteriorated beams and columns

- To renovate balcony bands

- To restore superficial concrete defects such as loose stone foundations, chipped parts, etc...

- To repair deteriorated concrete covers

- Repairing missing portions of screeds and plasters

- To level waterproofed surfaces with Plastivo and/or Aquascud

The material must have the following characteristics:

EC Certification according to EN 1504-3 - Class R3

Specification, Test method and Values

Flexural strength after 28 days (UNI EN 12190): 10.4 MPa

Compressive strength after 28 days (UNI EN 12190): 43.2 MPa

Adhesion to the concrete (UNI EN 1542): 1.62 MPa

Compressive modulus of elasticity after 28 days (UNI EN 13412): 20 GPa

Resistance to carbonation (UNI EN 13295): fulfilled requisite

Capillary absorption coefficient (UNI EN 13057): 0.14 kg*m⁻²*h⁻0.5

Thermal compatibility Part 1 (adhesion after 50 un/freezing cycles) UNI EN 13687-1: 2.41 MPa

Thermal compatibility Part 2 (adhesion after 30 thunder cycles) UNI EN 13687-2: 2.71 MPa

Thermal compatibility Part 4 (adhesion after 30 dry thermal cycles) UNI EN 13687-4: 2.50 MPa

as well as Flexomix 30 Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.

Per ulteriori dettagli sui singoli prodotti e specifiche di posa, fare riferimento alle relative schede tecniche scaricabili nella versione aggiornata sul sito internet www.volteco.com.

EN Specifications n. FF | CP | 01 | 01 | W | 07/26