GARVO due

Supply and installation of a joint cover strip made of a non-woven fabric with a central insert in thermoplastic rubber.

The product must be used in combination with modified polymer elastic mineral sheaths as a connection between adjacent surfaces and as a waterproof covering of structural lesions subjected to positive thrust.

The material must have the following characteristics:

Specification and Values

Working temperature: -30°C +90°C

Elongation at breaking point: > 37%

Tensile strength: > 235 N/5 mm

as well as GARVO due Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.

EN Specifications n. EE | CP | 00 | 01 | W | 07/26