PROCLEAN

Supply and installation of water-dispersed additive-based treatment with a disinfectant function, capable of neutralizing and protecting outdoor and indoor surfaces contaminated with mould, fungi and algae.

The product must be used for the preparation of mineral or synthetic substrates before the application of products such as Cp0, Cp1, Paint Air and Paint Protection, X-Lime and FibroeRaso or levelling products and paints in general, to both prevent and to remove deterioration caused by mould and algae.

The material must have the following characteristics:

Specification and Values

Appearance: whitish liquid

Specific weight: 1.1 kg/l

Viscosity (+20°C ≠ 2-100 rpm): 20 mPa x s

Workability time at +20°C: 30’

Application temperature: +5°C + 30°C

as well as Proclean Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.

EN Specifications n. EC254-EC255 | CP | 01 | 01 | W | 07/26