PROFIX 50

Supply and installation of water-based adhesion primer formulated with selected synthetic resins and additives, specifically for smooth, low-absorbent surfaces.

The product shall create a rough surface with high anchoring capacity, providing an ideal substrate for improving the adhesion of subsequent applications of liquid-applied elastic waterproofing membranes.

The material must have the following characteristics:

Specifications, Values

Appearance: dense liquid

Colour: grey

Application temperature: +5°C +35°C

Specific weight: 1.55± 0.05 Kg/l at 20 °C

Viscosity at 25±2°C: 8000 ± 1500 mPa s

Dry residue: 70 (±4) %

Drying time: 60' (*)

as well as Profix 50 Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and / or be

subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets

which can be downloaded in the updated version on the website www.volteco.com.

EN Specifications nr. CB13 | CP | 00 | 01 | W | 07/26