TAP 3

Supply and installation of quick-setting and hardening waterproof hydraulic mortar, ideal for quick, localised waterproofing works, even in the presence of pressurised water.

The product must be used for:
· Quick sealing of localised, pressurised water flows
· To rapidly prepare and finish waterproofing
· To seal cracks, together with hydro-expansive mastic Akti-vo 201



The material must have the following characteristics:


External temperature	at 20°C: Initial setting time 2’30” – Final setting time3’00”
External temperature	at 5°C: Initial setting time 5’20” – Final setting time 7’20

Specification, Test method and Values

Specific weight: >1,95 kg/l
Compress strenght (UNI EN 196-1)		after 1 hour: > 8 N/mm²
	after 1 day: > 18 N/mm²
	after 28 days: > 27 N/mm²
Flexural strength (UNI EN 196-1)	after 1 hour: > 1.5 N/mm²
	after 1 day: > 2.5 N/mm²
	after 28 days: > 3 N/mm²


as well as Tap 3 Volteco or a product with equal or superior characteristics.
The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.
For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.
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