WT 102

Supply and installation of hydro-expansive joint based on natural Sodium Bentonite and butyl rubber that seals construction joints in reinforced concrete structures, also in the presence of strong water pressure.

The product must be used for:

- To seal vertical and horizontal concrete construction joints

- To seal passing bodies embedded in the concrete castings

The material must have the following characteristics:

Specification and Values

Mixture composition (in weight): 25% butyl rubber; 75% Sodium Bentonite

Specific weight: 1.6 g/cm3

Application temperature: -15°C +50°C

Dimensions: 25x20 mm

Expansion due to contact with water (4 days): > 270%

Expansion due to contact with water: 701%

Swelling strain in total confinement: 966 kPa at 1000 hours

Swelling strain in sea water with total confinement: 978 kPa at 1000 hours

Hydraulic seal on 5 mm crack with expansion of 100%: No passage up to 100 kPa

as well as Wt 102 Volteco or a product with equal or superior characteristics.

The technical data must be supported by test certification issued by an accredited official laboratory and/or be subjected to quality control according to ISO 9001.

For further details on the individual products and installation specifications, refer to the relevant technical data sheets which can be downloaded in the updated version on the website www.volteco.com.

EN Specifications n. BD | CP | 00 | 01 | W | 07/26